## Slide 1
Texas State University PREM: Center on Interfaces in Materials. A Partnership the Research Triangle MRSEC
“Using Iron with Oxide Nanosheets to Enhance Electrochemical Lithium-Ion Charge Storage”
Research at Texas State University (MSI) and MSREC partner NC State demonstrated that iron oxide (g-Fe2O3) could be synthesized as a nanosheet architecture which resulted in significantly higher Li-ion capacities than nanoparticles; this work can provide enhanced cathodes for lower cost Li-ion batteries.
Niu, S.; McFeron, R.; Godínez-Salomón, F.; Chapman, B.S.; Damin, C.A.; Tracy, J.B.; Augustyn, V.; Rhodes, C.P. Enhanced Electrochemical Lithium-Ion Charge Storage of Iron Oxide Nanosheets, Chemistry of Materials, 2017, 29, 7794-7807
DMR-1205670
g-Fe2O3 nanosheet
g-Fe2O3 nanoparticle (commercial)
g-Fe2O3 nanosheets (TEM)
Iron oxide (i.e. rust) is very low cost but typically has a low capacity for storing Li-ions
Iron oxide can be synthesized as nanosheets
The iron oxide nanosheets are stabilized from transformation to nanoparticles by structural H2O and ethylene glycol
Iron oxide nanosheets have significantly higher capacities than nanoparticles
Nanosheet form allows surface-based charge storage
Furthers our ability to design low-cost cathodes for Li-ion batteries
Li+
e
Li+
e
Li+
e
g-Fe2O3 nanosheets (SEM)
g-Fe2O3 nanosheet
Notes: Iron oxides are appealing cathode materials for low-cost electrochemical energy storage, but iron oxide nanoparticles (NPs) exhibit very low capacities, particularly at fast charging and discharging times which are increasingly important for numerous applications.
We report that synthesis and stabilization of iron oxide in nanosheets results in significantly improved lithium-ion charge storage capacities compared to iron oxide NPs at both slow and fast charging/discharging times.
The transformation of γ-Fe2O3 from a nanosheet to a NP occurs in conjunction with removal of structural H2O and ethylene glycol.
The γ-Fe2O3 nanosheets exhibited lithium-ion charge storage capacities of up to 148 mAh g-1, which is significantly greater than commercial γ-Fe2O3 NPs (32 mAh g-1). γ-Fe2O3 nanosheets showed the ability to be rapidly charged and discharged (93.2 mAh g-1 at 9 min discharge times) with significantly higher capacities than γ-Fe2O3 NPs.
Kinetic analysis of the charge storage mechanism suggests the nanosheets store charge predominantly via a capacitive charge storage process rather than conventional intercalation.
The understanding of how to synthesize and stabilize iron oxide nanosheets, their unique electrochemical properties, and their distinct charge storage mechanism furthers the design of charge storage materials with improved capacities, enhanced rate capabilities, and lower cost.